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	Product Description
	A classic Polyurethane and Thixotropic  alkyd based Low Gloss Enamel , which has been especially formulated to give the best of long term performance/durability, Water and Steam resistance with no mess, non drip application properties it can used  for coating  a wide range of prepared house hold surfaces such as doors, window frames, cup boards etc in kitchens, Bathrooms and other high traffic areas  

	Application Areas
	· Hardboard and fibre cement boards.
· Primed metal and wooden substrates.


	Product Features
	· A high abrasion resistance, Low Gloss Durable Finish mostly for Interior use 
· Excellent adhesion and hiding power.
· Excellent water and steam resistance due to the presence of the Polyurethane 

· Excellent, no mess non drip application properties.
· Can be cleaned with normal house hold cleaners on a regular basis.

	Product Data
	Resin Base
	Synthetic Alkyd resin

	
	Drying Time
	Touch dry: 4-6 hours
Hard dry: 16-18hours

	
	Film Thickness
	± 30 microns

	
	Spreading Rate
	 8-10 SQM per 1 litre
Although the spreading rate will vary with porosity and type of substrate, for uncoated new surfaces work on 7-9 square metres per litre for the first coat and 9-11square metres per litre for subsequent coats and for when applied to sealed, previously painted substrates.

	
	Surface Appearance
	Low velvet like Gloss

	Application Details
	

	· Mixing
	Always stir well before use with a flat paddle.

	· Application Method
	· Brush, roller or spray application.

	· Thinning
	This is ready for use un-thinned; thinning with White Spirits will reduce its hiding power.

	· Cleaning
	Application equipment clean up is with White Spirits

	· Application
	· With brush, roller or spray, apply a generous coat of Paint Master High Gloss Enamel  to the area that needs protecting.
· Allow to dry overnight before recoating.
· Application equipment clean up is with White Spirits.
· Do not apply before 09:00 and after 16:00 in the winter.

	Surface Preparation
	

	· Rusted Metal
	· Remove any rust and mill scale from steel surface.

· Affected areas need to be cleaned back to bright metal 

· Apply one coat of Solvent or Water Based Metal Red Oxide , leave to dry over and apply a coat of Paint Master Universal Undercoat, allow to dry over night lightly  sand, wash off sand allow to dry .

· Apply two coats of Paint Master Non Drip Enamel.

	· New Metal
	· Degrease surfaces with an abrasive Degreaser to remove the manufacturer’s grease protective layer. This process is repeated until the surface is water break free.

· After drying Apply one coat of Solvent or Water Based Metal Red Oxide , leave to dry over and apply a coat of Paint Master Universal Undercoat, allow to dry over night lightly  sand, wash off sand allow to dry .

· Apply two coats of Paint Master Non Drip Enamel 

	· Dry, Uncoated Concrete Surfaces
	· Make sure concrete is firm and completely dry.

· Remove all dust, foreign material, fungal, algae growth.

· Fill all visible cracks with a suitable Crack Filler and allow to dry
· Seal repaired areas with Paint Master WB or SB Plaster Primer.
· Apply one coat of Paint Master WB or SB Plaster Primer
· Apply two coats of Paint  Master  Non Drip Enamel

	· Fibre Cement Surfaces (Uncoated, Weathered or New)
	· Remove dust, foreign material, fungal and algae growth.

· If friable or powdery, seal with Paint Master Bonding Liquid.

· Apply a Coat of Paint Master WB or SB Plaster Primer

· Apply 2 Coats of Paint Master Non Drip Enamel.


	· Raw Plaster
	· Make sure plaster is firm and completely dry.

· Remove all dust, foreign material, fungal and algae growth.

· Fill and seal all visible cracks and prime with Paint Master WB or SB Plaster Primer
· Apply two coats of Paint Master Non Drip Enamel

	· Previously Painted Surfaces
	· Make sure old paint coatings are firm and solid.

· Remove all loose, flaking and bubbling paint.

· Remove all dust, grease, foreign material, fungal and algae growth.

· If powdery or friable, seal with Paint Master Bonding Liquid.
· Prime with Paint Master WB or SB Plaster Primer.

· Apply two coats of Paint Master Non Drip Enamel.

	· Wood and Wood Fibre Boards
	· Sand surface until smooth.

· Apply one coat of Paint Master Universal Undercoat.
· Apply two coats of Paint Master Non Drip Enamel.

	Colour Range and Quantities
	· A wide range of Colours from The Paint Master Tinting system 
· Available in 1 litre, 5 litres and 20 Litres.

	Precautions
	· This product is flammable.
· Like all Alkyd or Oil Based Paints  This product will  have a tendency to change Colour/Yellow if it is painted in areas that get little or no natural  Sunlight or behind appliances (e.g. Fridges) that emit Ammonia  or Amines etc.

· Use only in well ventilated areas.

· Do not eat, drink or smoke while applying.
· This product continues no toxic substances.

	Disclaimer
	Martin Vosloo Paints can not be held liable if the product fails due to improper surface preparation or application.
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