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	Product Description
	Paint Master Hi-Cover is a new generation, cost effective, water based, good opacity matt paint for those areas where you want a matt finish to cover marks/imperfections.

	Application Areas
	· Primed wood/metal
· Primed cement,  plaster or fibre cement 
· Previously painted substrates



	Product Features
	· This matt paint hides plaster imperfections/marks on  walls 

· Good opacity

· Excellent adhesion
· Excellent, no mess application properties
· Low odor
· Quick drying 2 coats can be applied in one day

	Product Data
	Resin Base
	Acrylic resin emulsion

	
	Drying Time
	Touch dry: ± 1 hour
Hard dry: ± 4-6 hours

	
	Film Thickness
	25-35  microns per coat

	
	Spreading Rate
	6-8SQM per 1 litre

	Application Details
	

	· Mixing
	Always stir well before use with a flat paddle.

	· Application Method
	· Brush, Roller and Airless Spray 

	· Thinning
	This Product is ready for use un-thinned; thinning with water will reduce its hiding power.

	· Cleaning
	Clean application equipment with clean tap water.

	· Application
	· Stir well before use

· Apply a generous coat of Paint Master Hi-Cover with brush or roller, to the area that needs protecting

· Allow  to dry 3-4 hours before recoating

· Apply a second generous coat with a brush or roller 
· For best results use 2 coats of Paint Master Hi-Cover
· Product is ready for use un-thinned; thinning with water will reduce its hiding power

· Clean tools immediately after use with clean tap water
· Do not apply before 09:00 and after 15:00 in the winter


	Surface Preparation
	

	· Rusted Metal
	· Affected areas need to be cleaned to original condition. Prime the spot with Paint Master Water Based Metal Primer
· Remove collected sand and dust from the area
· Apply 2 coats of Paint Master Hi-Cover


	· New Metal
	· De-grease surfaces with a Galvanized Iron Cleaner to remove the manufacturer’s grease protective layer. This process is repeated until the surface is water break free
· Rinse well with potable water
· Prime  the clean, degreased metal  with the  Paint Master Water Based (WB) Metal Primer
· Apply 2 coats of Paint Master Hi-Cover

	· Wood 
	· Prime with  Paint Master Universal Undercoat 
· Lightly sand, wipe off dust

· Apply two coats of Paint Master Hi-Cover

	· Uncoated cement Plaster surfaces
	· Remove dust, foreign material, fungal and algae growth
· Fill all visible cracks and seal with Paint Master WB Plaster Primer
· Apply 2 coats of Paint Master Hi-Cover

	· Fibre Cement Surfaces (Uncoated, Weathered or New)
	· Remove dust, foreign material, fungal and algae growth
· If friable or powdery, seal with Paint Master Bonding Liquid or WB Plaster Primer
· Apply 2 coats of Paint Master Hi-Cover

	· Previously Painted Surfaces
	· Make sure old paint coatings are firm and solid
· Remove all loose, flaking and bubbling paint
· Remove all dust, grease, foreign material, fungal and algae growth
· Allow to dry
· If powdery or friable, seal with Paint Master Bonding Liquid or WB Plaster Primer 
· Apply 2 coats of Paint Master Hi-Cover

	Colour Range and Quantities
	· This Product is available in white and a limited range of  colours from the Paint Master Tint
· Available in 1, 5 and 20 litres

	Precautions
	· This Product is not flammable, contains no toxic substances and only low levels of VOC (EU regulations)

	Disclaimer
	Martin Vosloo Paints can not be held liable if the product fails due to improper surface preparation or application.
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