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	Product Description
	Paint Master Kitchen and Bathroom Sheen 

	Application Areas
	· Primed Wood/Metal
· Primed Cement  Plaster or Fibre Cement 
· Previously painted substrates.
· Mostly Interior (Kitchens + Bath Rooms-Where Water + Steam Resistance is essential)

	Product Features
	· This Product is a New Generation all Acrylic long Life Highly washable and Fungus Resistant Sheen
· Highly water/steam/stain and Fungus (mold) resistant.
· Excellent adhesion
· Excellent application properties.
· Low odour.
· Quick drying 2 coats can be applied in one day.

· Meets the Performance Criteria  of SABS 1586 Grade 1 

· A Special additive keeps the Fungus/Mold at bay  

	Product Data
	Resin Base
	Acrylic resin emulsion

	
	Drying Time
	Touch dry: ± 1 hour
Hard dry: ± 4-6 hours

	
	Film Thickness
	30-40  microns per coat

	
	Spreading Rate
	9-11 SQM per 1 litre
Although the spreading rate will vary with porosity and type of substrate, for uncoated new surfaces work on 8-10 square meters per litre for the first coat and 10-12 square meters per litre for subsequent coats and for when applied to sealed, previously painted substrates.

	Application Details
	

	· Mixing
	Always stir well before use with a flat paddle.

	· Application Method
	· Brush, Roller and Airless Spray 

	· Thinning
	This Product is ready for use un-thinned; thinning with water will reduce its hiding power.

	· Cleaning
	Application equipment clean up is with clean tap water.

	· Application
	· Stir well before use.
· Remove any mould or algae by washing the area with a mix of water and JIK or Spirit of Salts
· Let it dry and wash again with clean water

· Coat the area with two coats Paint Master Universal Undercoat
· With brush or roller apply a generous coat of Paint Master K+B sheen to the area that needs protecting.
· Allow to dry 3-4 hours before recoating.
· With a Brush or roller apply a second generous coat.
· 2 Coats of Paint Master K+B Sheen are used for best results.

· This Product is ready for use un-thinned; thinning with water will reduce its hiding power.
· Clean tools immediately after use with clean tap water.

· Do not apply before 09:00 and after 16:00 in the winter.
· Especially designed for Kitchens and Bathrooms

	Surface Preparation
	

	· Rusted Metal
	· Affected areas need to be cleaned back to bright metal and spot primed with Water based Metal Primer. 
· Remove collected sand and dust from the area.

· Apply two coats of Paint Master K+B Sheen


	· New Metal
	· Degrease surfaces with a Galvanized Iron Cleaner to remove the manufacturer’s grease protective layer. This process is repeated until the surface is water break free.

· Rinse well with potable water.

· Prime  the Clean Degreased Metal  with a water based Metal Primer
· Apply two coats of Paint Master K+B Sheen

	· Wood 
	· Prime With  Paint Master Universal Undercoat 
· Lightly Sand, wipe off dust

· Apply two coats of Paint Master K+B Sheen

	· Uncoated cement Plaster surfaces
	· Remove dust, foreign material, fungal and algae growth.

· Fill all visible cracks and seal with Paint Master WB Plaster Primer.

· Apply two coats of Paint Master K+B Sheen

	· Fibre Cement Surfaces (Uncoated, Weathered or New)
	· Remove dust, foreign material, fungal and algae growth.

· If friable or powdery, seal with Paint Master Bonding Liquid or WB Plaster Primer
· Apply two coats of Paint Master  K+B Sheen

	· Previously Painted Surfaces
	· Make sure old paint coatings are firm and solid.

· Remove all loose, flaking and bubbling paint.

· Remove all dust, grease, foreign material, fungal and algae growth.

· Allow to dry.

· If then powdery or friable, seal with Paint Master Bonding Liquid or WB Plaster Primer 
· Apply two coats of Paint Master K+B Sheen

	Colour Range and Quantities
	· This Product is available in white and a large range of  Colours from the Paint Master Tinting system  
· Available in 1, 5 and 20litres.

	Precautions
	· This Product is not flammable, contains no toxic substances and only low levels of VOC (EU regulations).

	Disclaimer
	Martin Vosloo Paints can not be held liable if the product fails due to improper surface preparation or application.
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