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	Product Description
	Paint Master Roof Paint 

	Application Areas
	· Primed wood/metal
· Primed cement, plaster or fibre cement 
· Previously painted substrates

·  Exterior 

	Product Features
	· New Generation, all acrylic, long life roof paint  
· Good durability and UV resistant for the harsh Gauteng climate

· Highly water resistance
· Excellent adhesion/flexibility
· Excellent, no mess application properties

· Quick drying 2 coats can be applied in one day
· If correctly applied to a properly prepared substrate, the product has a life expectancy of 5-7 years, possibly longer. The use of  a special polymer not only improves durability, but  also properties like water resistance and dirt shedding 

	Product Data
	Resin Base
	Acrylic resin emulsion

	
	Drying Time
	Touch dry: ± 1 hour
Hard dry: ± 4-6 hours

	
	Film Thickness
	30-40  microns per coat

	
	Spreading Rate
	6-8 SQM per 1 litre (depending on surface)

	Application Details
	

	· Mixing
	Always stir well before use with a flat paddle.

	· Application Method
	· Brush, Roller and Airless Spray 

	· Thinning
	This Product is ready for use un-thinned; thinning with water will reduce its hiding power.

	· Cleaning
	Application equipment clean up is with clean tap water.

	· Application
	· Stir well before use

· Apply a generous coat of Paint Master Roof Paint with a brush or roller to the area that needs protecting

· Allow 3-4 hours to dry before recoating

· Apply a second generous coat with a brush or roller
· For best results use 2 coats of Paint Master Roof Paint
· Product is ready for use un-thinned; thinning with water will reduce its hiding power

· Clean tools immediately after use with clean tap water
· Do not apply before 09:00 and after 15:00 in the winter
· Do not apply exterior if it looks like rain will occur within 4-6 hours of application

	Surface Preparation
	

	· Rusted Metal
	· Affected areas need to be cleaned to original condition. Prime the spot with Paint Master Water Based Metal Primer
· Remove collected sand and dust from the area
· Apply two coats of Paint Master Roof Paint


	· New Metal
	· Degrease surfaces with a Galvanized Iron Cleaner to remove the manufacturer’s grease protective layer. This process is repeated until the surface is water break free
· Rinse well with potable water
· Prime  the clean, degreased metal with a Paint Master Water Based (WB) Metal Primer
· Apply 2 coats of Paint Master Roof Paint 

	· Wood 
	· Prime with  Paint Master Universal Undercoat 
· Lightly sand, wipe off dust

· Apply 2 coats of Paint Master Roof Paint

	· Uncoated cement Plaster surfaces
	· Remove dust, foreign material, fungal and algae growth
· Fill all visible cracks and seal with Paint Master WB Plaster Primer
· Apply 2 coats of Paint Master Roof Paint 

	· Fibre Cement Surfaces (Uncoated, Weathered or New)
	· Remove dust, foreign material, fungal and algae growth

· If friable or powdery, seal with Paint Master Bonding Liquid  or Paint Master WB Plaster Primer
· Apply 2 coats of Paint Master Roof Paint

	· Previously Painted Surfaces
	· Make sure old paint coatings are firm and solid

· Remove all loose, flaking and bubbling paint
· Remove all dust, grease, foreign material, fungal and algae growth
· Allow to dry
· If then powdery or friable, seal with Paint Master Bonding Liquid or WB Plaster Primer 
· Apply 2 coats of Paint Master Roof Paint 

	Colour Range and Quantities
	· This Product is available in black, blue, bright blue, brown, charcoal, clay, custom grey, dark charcoal, desert, oak, muffin brown, green, platinum, plum, plum brown, red, tan, teasel grey, terracotta & white
· Available in 1, 5 and 20litres

	Precautions
	· This Product is not flammable, contains no toxic substances and only low levels of VOC (EU regulations)

	Disclaimer
	Martin Vosloo Paints can not be held liable if the product fails due to improper surface preparation or application.
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