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	Product Description
	Paint Master Ultra Matt

	Application Areas
	· Primed Wood/Metal
· Primed Cement  Plaster or Fibre Cement 
· Previously painted substrates.
· Interior or Exterior 

	Product Features
	· This Product is a New Generation all Acrylic long Life Paint Master Ultra Matt  
· Extremely durable and UV resistant for the harsh Gauteng climate.
· Highly water and Stain resistant., excellent polish resistance 
· Excellent adhesion/Flexibility
· Excellent, no mess application properties.
· Low odour.
· Hides plaster imperfections

· Quick drying 2 coats can be applied in one day.

· Meets most of the Performance Criteria  of SABS 1586 Grade 1 

· If correctly applied to a properly prepared substrate, the product has a life expectancy of 5-7 Years, possibly longer. The use of  a special polymer not only improves Durability but  also properties like water/polish resistance and dirt shedding 

	Product Data
	Resin Base
	Acrylic resin emulsion

	
	Drying Time
	Touch dry: ± 1 hour
Hard dry: ± 4-6 hours

	
	Film Thickness
	30-40  microns per coat

	
	Spreading Rate
	8-10 SQM per 1 litre

	Application Details
	

	· Mixing
	Always stir well before use with a flat paddle.

	· Application Method
	· Brush, Roller and Airless Spray 

	· Thinning
	This Product is ready for use un-thinned; thinning with water will reduce its hiding power.

	· Cleaning
	Application equipment clean up is with clean tap water.

	· Application
	· Stir well before use.
· With brush or roller apply a generous coat of Paint Master Ultra Matt to the area that needs protecting.
· Allow to dry 3-4 hours before recoating.
· With a Brush or roller apply a second generous coat.
· 2 Coats of Paint Master Ultra Matt are used for best results.

· This Product is ready for use un-thinned; thinning with water will reduce its hiding power.
· Clean tools immediately after use with clean tap water.

· Do not apply before 09:00 and after 15:00 in the winter.
· Do not apply exterior if it looks like rain will occur within 4-6 hours of application.

	Surface Preparation
	

	· Rusted Metal
	· Affected areas need to be cleaned back to bright metal and spot primed with Water based Metal Primer. 
· Remove collected sand and dust from the area.

· Apply two coats of Paint Master Ultra Matt


	· New Metal
	· Degrease surfaces with a Galvanized Iron Cleaner to remove the manufacturer’s grease protective layer. This process is repeated until the surface is water break free.

· Rinse well with potable water.

· Prime  the Clean Degreased Metal  with a Paint Master Water Based Metal Primer
· Apply two coats of Paint Master Ultra Matt

	· Wood 
	· Prime With  Paint Master Universal Under Coat 
· Lightly Sand, wipe off dust

· Apply two coats of Paint Master Ultra Matt

	· Uncoated cement Plaster surfaces
	· Remove dust, foreign material, fungal and algae growth.

· Fill all visible cracks and seal with Paint Master WB Plaster Primer.

· Apply two coats of Paint Master Ultra Matt

	· Fibre Cement Surfaces (Uncoated, Weathered or New)
	· Remove dust, foreign material, fungal and algae growth.

· If friable or powdery, seal with Paint Master Bonding Liquid or WB Plaster Primer
· Apply two coats of Paint Master Ultra Matt

	· Previously Painted Surfaces
	· Make sure old paint coatings are firm and solid.

· Remove all loose, flaking and bubbling paint.

· Remove all dust, grease, foreign material, fungal and algae growth.

· Allow to dry.

· If then powdery or friable, seal with Paint Master Bonding Liquid or WB Plaster Primer 
· Apply two coats of Paint Master Ultra Matt

	Colour Range and Quantities
	· This Product is available in white and a large range of  Colours from the Paint Master Tinting system  
· Available in 1, 5 and 20litres.

	Precautions
	· This Product is not flammable, contains no toxic substances and only low levels of VOC (EU regulations).

	Disclaimer
	Martin Vosloo Paints can not be held liable if the product fails due to improper surface preparation or application.
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