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	Product Description
	This Pigmented Plaster Primer is an unique water based penetrating, bonding and stabilizing primer for interior and exterior use on powdery, friable and very porous new and weathered substrates such as lime wash, old paint, new friable or porous plaster and fillers. Once the Paint Master WB Plaster Primer has done its job, these areas can be painted with a range of Paint Master Water and Alkyd based decorative products.



	Application Areas
	· Interior and exterior use

· New or weathered plaster, hardboard and fibre cement walls
· Powdery, friable, weathered, previously painted areas
· Lime wash

	Product Features
	· Unique water based product. The Primer penetrates deep into the substrate and stabilizes it
· Paint Master WB Plaster Primer is based on a resin emulsion and can therefore be diluted with water, which makes it a very cost effective product
· Martin Vosloo WB Plaster Primer has a good alkaline resistance and can be used on objects where aggressive minerals are present
· Once sealed the surface can receive a top coat with a wide range of Paint Master Water and Alkyd based products
· Excellent penetrating and binding properties
· Excellent adhesion. 

	Product Data
	Resin Base
	Synthetic polymer resin emulsion

	
	Drying Time
	Touch dry: ± 1 hour
Hard dry: ± 6-8 hours recoating time 8 hours for WB Top Coat overnight Dry for SB Top Coats Drying times will be lengthened in Cold or Damp conditions

	
	Film Thickness
	30-40  microns per coat

	
	Spreading Rate
	6-8  SQM per 1 litre

	Application Details
	

	· Mixing
	· Always stir well before use with a flat paddle

	· Application Method
	· Brush, Roller

	· Thinning
	· This Product is ready for use un-thinned; only thin with water if the substrate is extremely porous 

	· Cleaning
	· Clean application equipment immediately with clean tap water. If the Equipment dries, solvent will have to be used

	· Application
	· Stir well before use

· Apply a generous coat of Paint Master WB Plaster Primer with a brush or roller to the area that needs protecting

· Allow 6-8 hours for WB Paint to dry before recoating. Allow Solvent Based paint to dry overnight
· Consult Paint Master when Paint Master WB Plaster Primer is used as a base for Wall Paper
· Clean tools immediately after use with clean tap water
· Do not apply before 09:00 and after 15:00 in the winter
· Do not apply exterior if it looks like rain will occur within 6-8 hours of application

	Surface Preparation
	

	· Uncoated dry porous concrete surfaces
	· Remove dust, foreign material, fungal and algae growth
· Seal With Paint Master WB  Plaster Primer


	· Raw Plaster
	· Remove dust, foreign material, fungal and algae growth
· Seal with Paint Master WB  Plaster Primer

	· Uncoated, Weathered or New Fibre Cement Surfaces
	· Remove dust, foreign material, fungal and algae growth
· Seal with Paint Master WB Plaster Primer

	· Previously Painted Surfaces
	· Remove all loose, flaking and bubbling paint
· Remove all dust, foreign material, fungal and algae growth
· Lime wash coated walls: remove lime wash as far as possible with scraper blades and / or soft wire or hard fibre brushes but be careful not to damage the plaster.

· Allow to dry
· Fill and seal all visible cracks 
· Sand well and remove dust
· Seal with Paint Master WB Plaster Primer 

	Colour Range and Quantities
	· White 
· Available in 1, 5 and 20 litres.

	Precautions
	· This Product is slightly flammable, Flash Point 85-90 Deg C 

	Disclaimer
	· Martin Vosloo Paints can not be held liable if the product fails due to improper surface preparation or application.
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