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	Product Description
	New generation, water based non toxic anti-corrosive metal primer for use on degreased galvanised steel and rust free, clean and dry mild steel, under a range of Martin Vosloo Paints Decorative products. It is a very effective, anticorrosive metal primer.

	Application Areas
	· Degreased and/or weathered galvanized steel

· Rust free, clean, dry mild steel
· Sandblasted steel degreased galvanized metal and aluminum
· Highly recommended for high-corrosive areas such as coastal regions as well as in industrial environments and mines
· Can be used as an adhesion promoter on galvanised metal and as primer for old corroded zinc roofs

	Product Features
	· An anti-corrosive primer suitable for use in the harsh Lowveld environment

· Suitable for use on degreased galvanised steel and rust free mild steel

· Excellent adhesion
· Excellent, no mess application properties

· Can be over-coated with a range of Paint Master’s decorative products

· Low odor
· Based on a water-based resin and can be diluted with water. No thinner is required which makes the primer highly cost efficient
· This Product contains no lead or lead derivates, which makes this product environment friendly
· This Primer dries to a completely water insoluble, tough and abrasive resistant coating. The dry film thickness should not be less than 30 microns per coat. For coastal use we recommend a two-coat application. In the interior of the country one coat is sufficient

	Product Data
	Resin Base
	Acrylic Emulsion

	
	Drying Time
	Touch dry: 30–60 minutes


Hard dry: 2 – 3 hours

	
	Spreading Rate
	6.5 – 7.5 SQM per litre at 30 – 35 microns


	Application Details
	

	· Mixing
	Always stir well before use with a flat paddle.



	· Application Method
	Air or airless spray and with brush.

Roller application is not recommended.

	· Thinning
	Water (will reduce its hiding power and impair anti–corrosion protection).

	· Cleaning
	Water.

	· Application
	· Apply a generous coat of Paint Master Metal Primer with a brush, to the area that needs protecting
· In severe cases e.g. in very harsh marine environments, two coats of this Primer are required

· Allow 2-4 hours to dry before recoating with Paint Master Water Based products

· Allow 24 Hours to dry if using a Paint Master Alkyd Based Products as top coat
· This Primer is ready for use un-thinned, thinning with water will reduce its hiding power and impair anti–corrosion protection
· Clean application equipment with clean tap water
· This Primer should never be mixed with other products
· This Primer should never be used under two pack solvent or water based products
· Do not apply before 09:00 and after 15:00 in the winter
· Do not apply exterior if it looks like rain will occur within 4-6 hours of application

	Surface Preparation
	

	· Rusted Metal
	· Affected areas need to be cleaned to original condition by hand, mechanical or blast cleaning

· Apply 1-2 coats of this Primer by means of brush or spray application, but not by means of a paint roller

	· New Metal 
	· Degrease surfaces with an abrasive Galvanized Iron Cleaner to remove the manufacturer’s grease protective layer. This process is repeated until the surface is water break free
· After drying, the whole substrate is coated with 1-2 coats of this Primer

	Colour Range and Quantities
	· Red oxide only

· Available in 1/5lt (20lt on special order)

	Precautions
	· This product is not flammable.

· Contains no toxic ingredients and very low VOC levels (EU regulations).

	Disclaimer
	Martin Vosloo Paints can not be held liable if the product fails due to improper surface preparation or application.
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